SUPPORTING INFORMATION

A metal-enhanced Hg2+-responsive fluorescent nanoprobe: from morphological design to application to natural waters

Audrey Picard-Lafond,1,2 Dominic Larivière,1 Denis Boudreau1,2*

1Département de chimie and 2Centre d’optique, photonique et laser (COPL), Université Laval, Québec, QC

TABLE OF CONTENTS

1.	Isolation of DTC-FAM-SE and condensation attempt with APTES	1

2.	Physical properties of silica-based colloidal substrates	3

3.	Physical properties silver-cored colloidal substrates	5

4.	pH dependency	7

5.	Selectivity and interference study	7

6.	Real water sample data	8

7.	TCSPC-related data	9

8.	Additional schemes	9

# Isolation of DTC-FAM-SE and condensation attempt with APTES

DTC-FAM-SE was synthesized from commercial FAM-SE and PCTF. Briefly, in a 1.5 mL Eppendorf tube, 10 mg (21.1 μmol) of FAM-SE was dissolved in 150 μL of anhydrous MeCN. Then, 8.8 μL (63.6 μmol) of PCTF and 7.4 μL (42.5 μmol) of DIPEA were added to the FAM-SE solution. The reaction was mechanically stirred at 1000 rpm for 12 h. Upon solvent evaporation, the crude material was purified by column chromatography (silica gel, 50:50 ethylacetate:hexanes as eluent) to provide 10 mg (63%) of DTC-FAM-SE. HRMS (ESI): m/z calcd for C39H23NO11S2+H+: 746.0785 [M+H]+; found, 746.0772.

The synthetic conditions attempted to form DTC-Fl-APTES from DTC-FAM-SE were the following: In a 1.5 mL Eppendorf tube, 10 mg (13.4 μmol) DTC-FAM-SE was dissolved in 220 μL of DMF. Then, 3.1 μL (13.4 μmol) of APTES and 3.7 μL (26.8 μmol) of Et3N were added to the DTC-FAM-SE solution. The reaction was mechanically stirred at 1000 rpm for 3 h. The crude product was analyzed through mass spectroscopy, revealing a mixture of decomposition compounds as presented in Figure S1.

Scheme S1. Synthesis scheme of DTC-FAM-SE and DTC-Fl-APTES

Figure S1. Mass spectrum of the crude mixture obtained in attempt of converting DTC-FAM-SE to DTC-Fl-APTES, including identification of some of the decomposed structures generated.

# Physical properties of silica-based colloidal substrates

Figure S2. TEM images (left) and size distribution histograms (right) of (A) SiO2 NPs, (B) SiO2@Fl NPs and (C) SiO2@Fl-DTC NPs. Scale bars are 200 nm, d and N denote the average dry diameter calculated and number of particles analyzed, respectively.

Figure S3. Hydrodynamic size histograms of (A) SiO2 NPs, (B) SiO2@Fl NPs, (C) SiO2@Fl-DTC NPs and (D) dried and redispersed SiO2@Fl NPs obtained through NTA. The red error bars represent the standard deviation of four histogram replicates.

# Physical properties silver-cored colloidal substrates

Figure S4. TEM images (left) and size distribution histograms of cores and shells (center and right, respectively) of (A) Ag NPs, (B) Ag@SiO2 NPs (C) Ag@SiO2@Fl NPs and (D) Ag@SiO2@Fl-DTC NPs. Scale bars are 200 nm, d and l denote the core diameter and shell thickness calculated, respectively. N denotes the number of particles analyzed for each histogram.

Figure S5. Hydrodynamic size histograms of (A) Ag NPs, (B) Ag@SiO2@Fl NPs, (C) Ag@SiO2@Fl NPs and (D) Ag@SiO2@Fl-DTC NPs obtained through NTA. The red error bars represent the standard deviation of four histogram replicates.

Figure S6. Normalized extinction spectra of all Ag-core samples synthesized.

# pH dependency

Sample preparation for the pH sensitivity study proceeded as follows: 20 μL of a 50-µM stock solution of Hg2+ was added to 1.94 mL of HEPES buffer with a measured pH ranging from 3 to 10. The cuvette was then spiked with 40 μL of a (1.8 ± 0.1) x 1010 NP/mL suspension of Ag@SiO2@Fl-DTC NPs and a kinetic-based fluorescence acquisition was immediately performed for a total time of 60 s. The data was plotted as intensity versus time and the derivate was taken to report the kinetic rate r.

Figure S7. Normalized reaction kinetics of Ag@SiO2@Fl-DTC NPs with (red) and without (blue) 0.5 µM Hg2+ ions. Conditions: (3.6 ± 0.2) x 108 NP/mL dispersion in 20-mM HEPES buffer, 2% MeCN. Error bars represent RSD (n = 2).

# Selectivity and interference study

50-μM cation stock solutions were prepared from 1000-µg/mL standard solutions purchased from SPC Sciences. Sample preparation for the selectivity study proceeded as follows: 20 μL of a 50-µM stock solution of cation was added to 1.94 mL of HEPES buffer in a quartz cell placed in the spectrometer’s sample compartment. The cuvette was then spiked with 40 μL of a (1.8 ± 0.1) x 1010 NP/mL suspension of Ag@SiO2@Fl-DTC NPs and a kinetic-based fluorescence acquisition was immediately performed for a total time of 60 s. The data was plotted as intensity versus time and the derivate was taken to report the kinetic rate r. For the interference study, 20 μL and 80 µL of 50-µM stock solutions of Hg2+ and other cations, respectively, were added to 1.86 mL of HEPES buffer. The cuvette was then spiked with 40 μL of a (1.8 ± 0.1) x 1010 NP/mL suspension of Ag@SiO2@Fl-DTC NPs and the fluorescence measurements proceeded as stated above for the selectivity experiment.

Figure S8. Relative reaction kinetics of Ag@SiO2@Fl-DTC NPs in the presence of 0.5 µM of various cations (red bars) and 2 µM of various cations in combination with 0.5 µM Hg2+ ions (grey bars), where r0 is the rate of the cation-free conditions. Conditions: (3.6 ± 0.2) x 108 NP/mL dispersion in 20-mM HEPES buffer, pH 7.0, 2% MeCN. Error bars represent RSD (n = 2).

# Real water sample data

Table S1. Concentration of major ions (in mg/L) found in surface water (0-30 cm) of Lake Saint-Charles during ice-cover and open-water periods.1

| Ion | Ice-cover† | Open-water |
| --- | --- | --- |
| Ca | 7 | 6 |
| Cl | 19 | 13 |
| Na | 11 | 7 |
| Si | 3.4 | 2.4 |
| Al | 48 | 43 |
| Fe | 178 | 156 |

†Period spans from January to March, coinciding with frequent application of de-icing salts to nearby roads.

# TCSPC-related data

Table S2. Lifetime measurement data fitted through a two-exponential model

| Sample | A1 (%) | τ1 (ns) | A2 (%) | τ2 (ns) | τav (ns) | χ2 |
| --- | --- | --- | --- | --- | --- | --- |
| Fl-APTES† | 93.4 | 4.004 ± 0.009 | 6.6 | 1.93 ± 0.08 | 3.9 ± 0.2 | 1.030 |
| SiO2@Fl NPs* | 96.3 | 3.88 ± 0.02 | 3.7 | 0.0041 ± 0.0002 | 3.7 ± 0.2 | 1.311 |
| Ag@SiO2@Fl NPs* | 20.0 | 0.42 ± 0.02 | 79.0 | 0.0125 ± 0.0003 | 0.098 ± 0.007 | 3.614 |

† Decay curve for molecular Fl-APTES was fitted to a bi-exponential. *For particle-bound Fl, τ1 and τ2 terms were attributed to fluorescence and source scatter, respectively (Ag cores are highly efficient scatterers).

# Additional schemes

Scheme S2. Tautomeric forms of fluorescein and effect of functionalization with thionocarbonate moieties

9.  References

(1) 	Fournier, I. B.; Lovejoy, C.; Vincent, W. F. Changes in the Community Structure of Under-Ice and Open-Water Microbiomes in Urban Lakes Exposed to Road Salts. Front. Microbiol. 2021, 12, 1–12.

* Corresponding author: denis.boudreau@chm.ulaval.ca